## Slide 1: Leveraging NMR for Deformulation and Durability Assessment of Geosynthetic Materials Dr Frank Bambino and Dr John Scheirs

## Slide 2
Proton (hydrogen) NMR is a powerful solution phase spectroscopic technique for the identification and quantification of organic based polymer additives
Proton NMR is essentially a hydrogen atom detector
Signal response is directly proportion to the number of hydrogen atoms
Individual reference standards are not required for quantification of each analyte
All additives can be quantified in a single run
Perfect for the analysis of unknown samples

## Slide 3
High Performance liquid chromatography
Complementary technique to NMR spectroscopy for the quantification of polymer additives
Used in conjunction with NMR for complex samples enabling full characterization of polymer additives in geosynthetic materials (or any stabilised polymer material)
Polymer additives
HPLC Column with C18 coated silica adsorbent

## Slide 4
Polymer sample is exhaustively extracted with solvent to remove the additives
The isolated additives are dissolved prior to analysis
Accelerated Solvent Extraction (ASE)

## Slide 5
The dissolved additives are placed in glass tubes (0.8 mls) and inserted into the magnet bore.
NMR spectrometer
Superconducting magnet 600MHz (14 Tesla)
Radio frequency generator and detector
Sample Tubes

## Slide 6
Basic principle of NMR
When spins return to their lower energy state they release RF energy which is detected
The signal detected is called a free induction decay (FID)
NMR spectrum

## Slide 7
Typical Proton NMR spectrum of wine
201.4
300
4621.8
Chemical Shift (ppm)
Intensity
Can you Identify the components and assign the peaks?

## Slide 8
Proton NMR spectrum of wine
NMR spectrum
201.4
300
4621.8
Ethanol
Water
H2O
Wine is mainly ethanol and water
3H
2H
1H from ethanol
2H from water

## Slide 9
Proton NMR spectrum of Irganox 1010

## Slide 10
Proton NMR spectrum of Polymer extract
Irgafos 168 (oxidized)
Example polymer extract containing Irgafos 168, Irganox 1010, Irganox MD 1024 and Irganox 1330
MD 1024 Irg 1010 Irg 1330

## Slide 11
Failure analysis
Good sample
Failed sample

## Slide 12
Summary
NMR spectroscopy coupled with HPLC analysis are very powerful techniques for the deformulation of geomembrane materials.
Antioxidants and UV stabilisers can be identified and quantified.
Levels of plasticisers and Elvaloy can be identified and quantified
NMR analysis is well suited to the analysis of unknown additives in geomembrane samples (e.g. competitor analysis)
Troubleshooting in failure analysis
Fin (end)